## Slide 1
计算物理模拟实验
助教：武思怡
Email: 23210190041@m.fudan.edu.cn
课程微信群
授课人：龚新高 褚维斌
Email: xggong@fudan.edu.cn wbchu@fudan.edu.cn
办公室： 江湾校区交叉一号楼A4007

## Slide 2
Project 1 理论课
Project 1 汇报
Project 2 理论课
Project 2 汇报
课程安排
时间：周六上午9点
地点：江湾校区交叉一号楼A5005
Project 1 进展总结
Project 2 进展总结
其余时间每周六为答疑时间

## Slide 3
课程考核
课题汇报 (50%)
程序 +实验报告 (45% ) 截止日期： 每次课题汇报后一周
课程反馈 （5%）
旨在借助计算模拟的方法去加深对物理学的重要知识点的理解，对编程技巧不做考核，鼓励使用AI，但注意AI可能会误导！

## Slide 4
实验目的
1. 了解固体力学性质和原子键合关系
2. 掌握弹性常数等力学量的计算方式
3. 理解弹性波在晶体中的传播
4. 认识温度对力学性能的影响
实验内容
基于原子间相互作用势编写程序计算模拟金属铝和绝缘体金刚石的零温和有限温下的力学性质。并思考分析以下问题：
  思考不同化学键对弹性常数以及物理性质的影响，分析计算误差来源与如何降低误差。探索不同晶系的独立矩阵元是否有不同。
  基于弹性常数计算两种体系的各种力学量和固体性质，模拟不同晶体中弹性波在[100]、[110]、[111]方向的传播，观察横波和纵波的区别。
晶体弹性模拟计算实验

## Slide 5
  模拟金刚石不同温度下的弹性常数，观察不同弹性常数随温度变化的趋势。
  模拟不同的Strain大小对应的Stress， 得到Strain-Stress relation，思考在多大的范围内胡克定律成立？

## Slide 6: Elasticity
Important because most engineering design is done in the elastic region. (Remember, plastic deformation generally constitutes failure.)
Macroscopically, most polycrystalline materials are elastically isotropic.
Microscopically, elastic behavior is inherently anisotropic for individual grains.
Polycrystalline materials can be anisotropic if they exhibit strong crystallographic textures.

## Slide 7
Derived from atomic bonding forces originating from long range attractive forces which draw atoms together until short range repulsive forces become large enough to balance them out.
As such, elastic properties are an aggregate effect of individual deformations of interatomic bonds.
Repulsion
Attraction
ro
r
U
F
r
r
o
F = -dU/dr
F is maximum at point of inflection in U/r curve
Elasticity

## Slide 8: Bulk Elastic Behavior
Applied force is transmitted by the network of bonds constituting the material.
Thus, elastic behavior depends quantitatively on the magnitude of the interatomic forces.
Elastic properties do not depend on microstructure of the material.

## Slide 9: Forces Between Atoms
Bonds form when atoms either share (e.g., covalent and metallic bonds) or transfer (e.g., ionic bonds) electrons between atoms.
This occurs to achieve a minimum in potential energy for the system corresponding to a stable electron configuration.
This has been modeled for ionic systems as follows:

## Slide 10: Ionic Bond
Electron transfer from one atom to another occurs due to electrostatic interaction between oppositely charged ions (e.g., Na+ and Cl- in NaCl).
Force of attraction between ions is Fattract
Work is done to draw ions together. It is given by:
+
-
r
q2
2
q  charge of ion
r  ionic separation distance
o
  permittivity of free space
Fattract
o
4 r

r
Uattract
attract
m
o
4 r r
q2  A

 F
dr 



## Slide 11
Each atom maintains an electron cloud surrounding it. The outer surfaces of each atom are both negatively charged.
Thus, at close distances, the electron clouds overlap and repel. The repulsive force can be written as:
This is the well known Lennard-Jones potential. You might recall this from your chemistry or physics courses.
repel
rn
 B
U
The total energy of the system is thus the sum of the attractive and repulsive components. It can be expressed in general as:

## Slide 12
The minimum energy point corresponds to the equilibrium separation (i.e., the equilibrium bond length, ro).
The bond stiffness is the derivative of the force versus distance plot.
Repulsion
Attraction
ro
r
U
F
dr
The force between atoms is simply the derivative (i.e., the slope) of the energy versus distance plot.
F  dUtotal
r
ro
dF d 2U
dr dr 2
 total
S 

## Slide 13
At the equilibrium bond length, ro, the variation of F with r is essentially linear, which means that the stiffness is essentially constant at small distances from ro.
ro
o
S
dr
 dF
Using this expression, the force to “stretch” n bonds in a solid is:
r
F  n Sodr  nSo r  ro 
ro
where n is the number of bonds.

  The applied stress is:
ro
o
r
o
r

## Slide 14: The derived expression shows that the modulus is dependent upon bonding.
The strain can be expressed as:
  r  ro
Thus, stress becomes:
From Hooke’s law:
  E
Thus,
ro
2
S 1 d 2U
o
E  o
ro ro dr
r r

Modulus, and other elastic properties, are
structure insensitive.
The directionality of elastic properties does depend upon atomic arrangement (crystallography) in single crystals. They tend to average out in polycrystals.


## Slide 15
[From W.D. Callister, Jr, Materials Science and Engineering: An Introduction, 7th Ed., (Wiley, New York, 2007) p.28]
Bonding Type | Material, Substance | Bonding Energy |  | Melting Temperature °C
 |  | kJ/mol | eV/Atom, Ion, Molecule | 
Ionic | NaCl | 640 | 3.3 | 801
 | MgO | 1000 | 5.2 | 2800
Covalent | Si | 450 | 4.7 | 1410
 | C (diamond) | 713 | 7.4 | >3550
Metallic | Hg | 68 | 0.7 | -39
 | Al | 324 | 3.4 | 660
 | Fe | 406 | 4.2 | 1538
 | W | 849 | 8.8 | 3410
van der Waals | Ar | 7.7 | 0.08 | -189
 | Cl2 | 31 | 0.32 | -101
Hydrogen | NH3 | 35 | 0.36 | -78
 | H2O | 51 | 0.52 | 0

## Slide 17
Young’s modulus, GPa
Steel Copper Aluminum Zinc Lead Metals | PEEK PP PTFE Polymers | WC Alumina Glass Ceramics | CFRP GFRP Fibreboard Composites
Ceramics
The elastic
classes of materials (i.e., metals, ceramics, polymers and composites). tend to exhibit the highest elastic moduli and polymers the lowest. moduli of composites are between those of their constituents.
Courtesy of Granta Design
A bar chart illustrating Young’s moduli for some common examples of the primary
Covalent or Ionic bonding
Metallic bonding

## Slide 18: stress is related to strain for an isotropic solid
Hooke’s Law
– Isotropic Solids (properties are the same in all directions)
Anisotropic solids (properties are directional)
Need different definition
Let’s consider both cases
Load
Unload
Slope = E (Modulus of elasticity)
Stress-strain plot for a linearly elastic material
Strain
Stress
0
0
E
   E or   1 

## Slide 19: First consider the Poisson effect
lateral strain
Poisson's Ratio,   
longitudinal strain
unloaded
x
y
z
F
loaded
 (z, x)    x and  (z, y)    y
 z  z
A tensile stress along the z axis causes the material to stretch along the z axis and to contract along the x and y axes.

## Slide 20
Room- Temperature Poisson’s Ratio for Selected Solids
Material Class | Material | 
Metallic solid | Ag | 0.38
(crystalline) | Al | 0.34
 | Au | 0.42
 | Cu | 0.34
 | -Fe | 0.29
 | Ir | 0.26
 | Ni | 0.31
 | W | 0.29
Covalent solid | Ge | 0.28
(crystalline) | Si | 0.27
 | Al2O3 | 0.23
 | TiC | 0.19
Covalent Ionic Solid | MgO | 0.19
Covalent Glass | Silica glass | 0.20
Network Polymer | Bakelite | 0.20
 | Ebonite (hard rubber) | 0.39
Elastomer | Natural rubber | 0.49
Chain Polymer | Polystyrene | 0.33
 | Polyethylene | 0.40
Van der Waal’s Solid | Argon (at 0 K) | 0.25

## Slide 21
The strains resulting from this stress state must be the sum of the strains associated with loading along each individual axis.
B
xx
B B
yy
C
yy
C
B
xx
C
xx
B: 
C: 
xx
xx
yy
C
xx
yy
xx
A  B+C :   
E
E
E
E
E
  xx
E
  yy


 

 
,      xx
 
 ,      yy
 xx
 xx
 yy
yy

 xx
 xx
 yy
yy
 C
A
B
There’s a similar expression for εyy

## Slide 22: Elastic Stress-Strain Relations
Stress
Strain in the x-direction
Strain in the y-direction
Strain in the z-direction
Variation in elastic strain for an isotropic solid because of the Poisson effect
xx

xx
E
  xx

 xx
 yy  E
 xx
 zz  E
yy

 yy
 xx  E
E
 yy
 yy 
 yy
 zz  E
zz

 zz
 xx  E
 zz
 yy  E
 zz
 zz  E
 xy  G xy ;  yz  G yz ;  xz  G xz

## Slide 23: Other Elastic Stress-Strain Relations for Isotropic Solids
Bulk Modulus (K), also known as the volumetric elastic modulus:
K  hydrostatic pressure   m   p  1 volume change produced   B
where:
- p  hydrostatic pressure,
3
  zz ,
  xx   yy   zz
  dilatation (i.e., volume change)   xx
B  compressibility.
m
  yy


## Slide 24
Now we can relate the elastic constants.
Summation yields:

Other Elastic Stress-Strain Relations for Isotropic Solids

## Slide 25
In terms Elastic constants | E, ν | E, G | K, ν | E, G | λ, μ
E [elastic] | = E | = E | = 31  2  K | = 9K 1  3K / G |  3  2 /   = 2 1   /  
ν | = ν | = 1  E 2G | = ν | = 1  2G / 3K 2  2G /3K | 1 = 2 1   /  
G [shear] | E = 2 1   | = G | 31  2  K = 2 1   | = G | = μ
K [bulk] | E = 31  2  | = E 9  3E / G | = K | = K | =   2 3
λ | E = 1  1  2  | = E 1 2G / E  3  E / G | = 3K 1  | = K  2G 3 | = λ
μ | E = 2 1   | = G | 31  2  K = 2 1   | = G | = μ
λ, μ = Lame constants
Other Elastic Stress-Strain Relations for Isotropic Solids

## Slide 26
Energy stored in a body due to deformation.
Work to deform a body elastically is stored as elastic strain energy. It is recovered when the applied forces are released.
Strain energy is proportional to the area under the load- deformation (stress-strain) curve.
We will elaborate on this concept on the next
few pages.
Deformation δ
Load F
2
U  1 F
Elastic Strain Energy

## Slide 27
The first law of thermodynamics states:
dU   Q  W  TdS  PdV
where,
dU = internal energy
δQ = heat
δW = mechanical work done
During elastic deformation, the amount of heat generated is negligible.
Thus the work done on the body is converted into internal energy and is fully recovered upon unloading.
Elastic Strain Energy

## Slide 28
Consider an elemental cube that is subjected to only an elastic tensile stress along the x-axis. The elastic strain energy, U, is:
2
U  1 (load)(deformation)
1 1
1
= total elastic energy absorbed by the material element.
dU  Fdu   xx A xx dx   xx xx  Adx
2 2 2
Since Adx is the volume, the elastic strain energy per unit volume (i.e., the strain energy density) is:
o
xx xx
dU 1
Adx 2
   .
U 
 xx
A
xx
F
 xx  A
 du
dx

x
y
z
Elastic Strain Energy

## Slide 29
2
2
2
2
From Hooke's law,
Therefore:
1
1
1
In three dimensions, the general expression for elastic strain energy is:
1
2
xx
Uo 
xx
1  1
2 E 2
  E [in tension]
xy
o xy xy
xy
2 2 G 2
U     
  G [in pure shear]
Uo 
 xx xx   yy yy   zz zz  xy xy  xz xz

 yz yz .
 xx
A
xx
xx
 F
A
 du
dx


x
y
z
Elastic Strain Energy

## Slide 30
2
ij
2
In tensor notation, these general expressions become:
1 1
1
If we substite into these expressions, the variation in elastic strain for an isotropic solid, accounting for the Poisson effect, we get:
o ij ij
ij
2 2 E 2
U    
  E.

 
 


 


2
xx
2
xy
  2   2
xz yz
2
xy
2
xz
2
yz
1
1
2E
2G
[for a 3D isotropic solid]
Expressed in terms of strains and elastic constants:
1
2
2
o
yy
2
zz
xx yy
yy zz
xx zz
o
2
xx
2
yy
2
zz
U  1 2  G 
U 
 G 

  2  
 
E
        

 
 
   
Elastic Strain Energy

## Slide 31
The derivative of Uo with respect to any strain component yields the corresponding stress component, or:
Similarly, the derivative of Uo with respect to any stress component yields the corresponding strain or:
Uo
ij
   2G  
ij
ij

You can use these terms to calculate stresses and strains in elasticty. Techniques for doing this include Castigliano's theorem, the theorem of least work, and the principal of virtual work.
Uo
ij
ij
 

Elastic Strain Energy

## Slide 32: Anisotropy and Single Crystals
They act along the “lines” connecting the atoms together.
Forces between atoms are directional.
(110)BCC

## Slide 33: Relations between stress and strain for anisotropic crystals
Since force varies with direction, elastic constants will also vary.
In general, we need to relate every stress component to every strain component.
Thus we must define two new elastic constants:
  C  stiffness
  S  compliance
We also re-write Hooke’s law as:
 ij  Cijklkl or ij  Sijkl kl

## Slide 35: Allow us to reduce the number of constants from 81 to 36
 ij   ji Cijkl  C jikl Cijkl  C jikl
kl Cijkl Cijkl
 lk
 C jikl
 Cijlk
zz
yyxx
yyyy
Cxxyy
yyzz
Cxxzz
yyyz
Cxxyz
yyxz
Cxxxz
zzxx
 xx 
Czzyy
Czzzz
Czzyz
C
C
C
C
C
Cxxxy   xx 

yy 
  
 


yz 
  xz 

xy 
EQUILIBRIUM CONSIDERATIONS
yzxx
yzyy
yzzz
yzyz
yzxz
Czzxz
xyxx
 Cxxxx
   C
xyyy
Cxzyy
xyzz
Cxzzz
xyyz
Cxzyz
xyxz
Cxzxz
C
C
C
C
C
Czzxy   zz 
C
C
C
C
C
xyxy  xy 
Cxzxy   xz 
  
yyxy  yy 
  
yzxy  yz 
  

 C
 C

 Cxzxx
   C


## Slide 36:  xx 
yyxx
yyyy
Sxxyy
yyzz
Sxxzz
yyyz
Sxxyz
yyxz
Sxxxz
zzxx
yzxx
yzyy
Szzyy
yzzz
Szzzz
yzyz
Szzyz
yzxz
Szzxz
Sxzyz
Sxzxz
xyxx xyyy
zz
Sxzyy
Sxzzz
S
S
S
S
S
Sxxxy  xx 
S
S
S
S
S
Szzxy   zz 
S S

  xx 

yy 



yz 
  xz 

xy 
xyzz
 Sxxxx
    S
xyyz
xyxz
S
S S
Sxzxy   xz 
 
yyxy  yy 
 
yzxy  yz 
 
xyxy  xy 

  S
    S

 Sxzxx
    S

yyxx
yyyy
Cxxyy
yyzz
Cxxzz
yyyz
Cxxyz
yyxz
Cxxxz
zzxx
yzxx
yzyy
Czzyy
yzzz
Czzzz
yzyz
Czzyz
yzxz
Czzxz
Cxzyz
Cxzxz
xyxx
xyyy
Cxzyy
Cxzzz
zz
C
C
C
C
C
Cxxxy   xx 
C
C
C
C
C
Czzxy   zz 
C C
xyzz

 

yy 



yz 
  xz 

xy 
 Cxxxx
 C
xyyz
xyxz
C
C C
Cxzxy   xz 
  
yyxy  yy 
  
yzxy  yz 
  
xyxy  xy 

  C
   C

 Cxzxx
   C

 ij  Cijklkl
ij  Sijkl kl
Sijkl is the COMPLIANCE matrix
Cijkl is the STIFNESS matrix
 xz 

## Slide 37: Matrix/Contracted Notation
We often replace the indices with matrix (contracted) notation for simplicity [Voigt, Lehrbuch der Kristallphysik (Teubner VErlag, Berlin, 1910)].
Thus, Hooke’s law is often re-written in matrix form as:
 p  Cpqq or  p  Spq q
xx  11  1
yz  23  4
yy  22  2
xz  13  5
zz  33  3
xy  12  6
11 12 13   1 6 5 
 22 23   2 4 

33
 3 
   
row
column

## Slide 38: Additional note about contracted notation
Numbers 1-3 are associated with normal stresses and strains.
Numbers 4-6 are associated with shear stresses and strains.
On the next slide I attempt to show you which stresses and strains are related to each elastic constant.
x
z
y
4
3
1
2
5
6
4
5
6

## Slide 39
yzyz
yzxz
xyyz
xyxz
yyxx
yyyy
yyzz
yyyz
yyxz
yzxx
yzyy
yzzz
xyxx
xyyy
xyzz
Cxxzz
Cxxyz
ijkl
C
C
C
C
C
Czzyy
Czzzz
Czzyz
Czzxz
C
C
C
C
C
C
Cxzyy
Cxzzz
Cxzyz
Cxzxz
C
C
C
C
C
 ,
Cxxyy
 ,
Cxxxz
 Cxxxx
 C

  Czzxx
 C

 Cxzxx

Cxxxy 
 ,
 ,

yyxy 
Czzxy 

yzxy 
Cxzxy 
 C

xyxy 
21
22
23
24
25
44
45
41
42
43
ijkl
C C C C C
C
C C C C C
C C C C C
 C11
 ,  ,
C12 C13 C14 C15 C16 
 C


26 
  C31 C32 C33 C34 C35 C36 
 C


46 
 C51
 C

C52 C53 C54 C55 C56 
 61 62 63 64 65 66 
 ,  ,
TENSOR
CONTRACTED

## Slide 40: Contracted vs. Tensor Notation
Contracted notation is simple and convenient for conducting matrix inversions.
However, for coordinate transformations or invariant determination, it is more useful to use the stiffness and compliances in tensor notation.

## Slide 41
21
22
23
24
25
41
42
43
44
45
61
C C C C C
C32 C33 C34 C35
C C C C C
C52 C53 C54 C55
62 63 64 65
C
C C C C
 C11 C12 C13 C14 C15
 C

 1 
C16  1 
 
  

2 
26  2 
 

4 
 3    C31
C36  3 
 C
  

 C51
 C

46  4 
 5 
C56  5 
 
  

6 
66  6 
S S S S S
S32 S33 S34 S35
S S S S S
S S S S S
 S11 S12 S13 S14 S15
 S

 1 
S16  1 
  
 

2 
21 22 23 24 25 26  2 

4 
 3    S31
S36  3 
    S
 

 S51 S52 S53 S54 S55

41 42 43 44 45 46  4 
 5 
S56  5 
    S
 

6  61 62 63 64 65 66  6 
 p  Cpqq
 p  Spq q
Spq is the COMPLIANCE matrix
Note the change from tensor notation to matrix notation. See Chapter 8 in Nye for details.
Cpq is the STIFNESS matrix

## Slide 42: Stiffness and compliance matrices are also symmetric about the main diagonal
Required number of components reduces to 21
The number can be further reduced by considering crystal symmetry
21
22
23
24
25
22
23
24
25
36
41
42
43
44
45
44
45
61
C12
C13
C14
C15
C C C C C
C C C C C
C
C C C C C
 C11
C16 
 C
C
C C C C
C52 C53 C54 C55 C56 
62 63 64 65

26 
 C31 C32 C33 C34 C35

 C


46 
 C51
 C

66 

 C11 C12 C13 C14 C15 C16 
  

26 

  
 

46 
 

 C33 C34 C35 C36 
   C C C
    
  
C55 C56 
 C

66 
21
22
23
24
36
41
42
43
44
61 62 63 64
S
S S S S S
S
S12 | S13 | S14 | S15
S | S | S | S25
S32 | S33 | S34 | S35
S | S | S | S45
S52 | S53 | S54 | S55
S | S | S | S65
S
 S11
S16 
 S

 S31

 S

46 
 S51
S56 
 S
 S11 S12 S13 S14 S15 S16 

22 23 24 25 26 
  

44 45 46 
  

  
26  
S     S33 S34 S35 S36 
   S S S
    
  
S55 S56 
 S
 66   66 

## Slide 43: Neumann's Principle
“The symmetry of any physical property of a crystal must include the symmetry elements of the point group of the crystal.”
Point groups are the group of macroscopic symmetry elements possessed by the structure of a crystal.*
Crystals exhibit specific point symmetries.
Crystal “properties” will include the point group but can exhibit more symmetry than the point group.
* Review pages 20-25 and 279-288 in Nye for a more complete treatment.

## Slide 44: Possible Macroscopic Symmetry Elements
Center of symmetry
Mirror plane
1-, 2-, 3-, 4- or 6-fold rotation axes
1-, 2-, 3-, 4- or 6-fold inversion axes

## Slide 45
Symbolism for the symmetry elements of the 32 point groups
[Table from J.F. Nye, Physical Properties of Crystals, (Oxford University Press, Oxford, 1985) p. 280]
Crystal systems
The 32 crystal classes (i.e., point groups) are conventionally grouped into seven crystal systems.
The requirements for membership in a given crystal system is that the symmetry of the class should possess a certain minimum characteristic.

## Slide 46
Cubic
Hexagonal
120°
Tetragonal
Rhombohedral
Orthorhombic
Monoclinic
Triclinic
We can describe shapes and arrangements of points within shapes in terms of the symmetry exhibited by them.
In crystal systems, the symmetry of a class of crystals should possess a certain characteristic symmetry (i.e., certain minimum symmetry elements).

## Slide 47: We describe crystal symmetry relative to specific crystallographic axes and symmetry elements operating on those axes
Table adapted from R. Tilley, Crystals and Crystal Structures, John Wiley & Sons, Hoboken, NJ, 2006, p. 73.
Tertiary
The order of Hermann-Mauguin symbols in point groups
Crystal System Primary Secondary
Monoclinic
Orthorhombic
[001]
Tetragonal
Triclinic  

[010], unique axis b 
[001], unique axis c

[100] [010]
[001] [100], [010]
[1 10], [110]
Trigonal, Rhombohedral Axes
[111]
[1 10], [011], [101]
Trigonal, Hexagonal Axes
[001]
[100], [010], [110]
Hexagonal
[001]
[100], [010], [1 10]
[1 10], [120, [210]
Cubic
[100], [010], [001]
[111], [1 11], [11 1], [1 11]
[1 10], [110], [01 1],
[011], [101], [101]
The concept of crystal symmetry is illustrated on the next six viewgraphs.
You should review this and related literature on your own time.

## Slide 48
2-fold rotation.
Rotation about the center point.
1
180° rotation moves point “1” to “2” but produces same pattern.
Second 180° rotation moves original point (labeled with a “1”) back to its starting point.
2

## Slide 49
43m
4-fold inversion axes parallel to x,y,z
(aka, <100>)
3-fold rotation axes parallel to cube diagonals
(aka, <111>)
Mirror plane parallel to face diagonals (aka, <110>)
Tetrahedron inscribed in a cube
Symmetry elements in a regular tetrahedron. (a) tetrahedron inscribed in a cube showing three Cartesian axes; (b) 4-fold inversion axes along x [100], y [010] and z [001]; (c) 3-fold rotation axes passing through vertex and center of opposite triangular face (i.e., [111]); (d) mirror planes parallel to [110]. Adapted from Fig. 4.6 in R. Tilley, Crystals and Crystal Structures, John Wiley & Sons, Hoboken, NJ, 2006.

## Slide 50
43m
Octahedron inscribed in a cube
4-fold rotation axes parallel to x,y,z (aka, <100>) with perpendicular mirror plane.
3-fold inversion axes parallel to cube diagonals (aka, <111>)
2-fold rotation axes parallel to face diagonals
(aka, <111>) with perpendicular mirror plane.
R. Tilley, Crystals and Crystal Structures, John Wiley & Sons, Hoboken, NJ, 2006.

## Slide 51: We describe lattice shapes and arrangements of lattice points in the same way.

## Slide 52: Symmetry of the Cubic P-Lattice
Adapted from W. Borchardt-Ott, Crystallography, 2nd Edition, (Springer, Berlin, Germany, 1995) p. 99
Primary
Secondary
Tertiary
Letter symbol

P 4 m 3 2 m
  
100 111 110
Four 3-fold rotation axes parallel to cube diagonals
(aka, <111>)

## Slide 53
[Nye, p. 284]
There are only 32 crystal classes derived from the 7 crystal systems (i.e., shapes).
Each has a certain characteristic symmetry.
They are presented on stereograms on this viewgraph and the two that follow.
Table 21.3
Triclinic
Monoclinic
Orthorhombic
Table 21
Symmetry elements and conventions for the choice of axes in the 32 crystal classes
Symbols of centrosymmetrical classes are enclosed in boxes

## Slide 54
[Nye, pp. 285-286]
Table 21.2
Tetragonal
Table 21.3
Trigonal

## Slide 55
[Nye, pp. 287-288]
Table 21.4
Hexagonal
Table 21.5
Cubic

## Slide 56: Influence of Crystal Symmetry on Number of Elastic Constants
Crystal System | Axial Relation- ships | Interaxial Angles | Minimum Symmetry Elements | Number of Elastic Constants
Cubic | a = b = c |  =  =  = 90° | Four 3-fold rotation or rotoinversion axes parallel to body diagonals | 3
Hexagonal | a = b ≠ c |  =  = 90°;  = 120° | One 6-fold rotation or rotoinversion axis parallel to z-axis | 5
Tetragonal | a = b ≠ c |  =  =  = 90° | One 4-fold rotation or rotoinversion axis parallel to z-axis | 6 or 7
Rhombohedral (Trigonal) | a = b = c |  =  =  ≠ 90° | One 3-fold rotation or rotoinversion axis parallel to z-axis | 5, 6 or 7
Orthorhombic | a ≠ b ≠ c |  =  =  = 90° | Three 2-fold rotation or rotoinversion axes parallel to x,y,z-axes | 9
Monoclinic | a ≠ b ≠ c |  =  = 90° ≠  | One 2-fold rotation or rotoinversion axis parallel to y-axis | 13
Triclinic | a ≠ b ≠ c |  ≠  ≠  ≠ 90° | - None - One 1-fold rotation or rotoinversion axis | 21
Increasing crystal symmetry
Increasing # Elastic const.

## Slide 57: Reduction of Elastic Constants with Increasing Symmetry
A clear explanation of the reduction in the number of elastic constants due to crystal symmetry is provided in Chapter 6 of Wagoner and Chenot (pp. 196-207).
Excellent explanations are also provided in Nye (i.e., Ch. 8 and Appendix B) and in Reid (Ch. 3).
You are urged, but not required, to review some of this material.

## Slide 58
Form of the elastic constant matrices for different symmetries
Zero component (s = 0, c = 0)
Non-zero component (s ≠ 0, c ≠ 0) Equal components
Numerically equal but opposite
 = 2 for s;  = /2 for c
=2(s11 – s22) or (c11 – c22)/2
Figure adapted from J.F. Nye, Physical Properties of Crystals, Oxford University Press (1985), p. 140-141.

## Slide 59: Cubic Symmetry and Elastic Constants
Application of a stress along the [100] direction evokes a certain elastic response. Stresses applied along the [010] or [001] axes will evoke an equivalent elastic response. Thus:
–
C11 = C22 = C33
Similarly, applied shear stresses will evoke equivalent responses along the following axes:
–
C44 = C55 = C66; C12 = C13 = C23
The number of independent elastic constants for a cubic material is 3.
3
2
1

## Slide 60: Isotropy considerations
When the Zener ratio = 1, the material is isotropic.
NOTE: Some books (Ex., Hertzberg) present an inverted version of this equation. However, the implications are still the same.
3
2
1
Cubic materials are not necessarily isotropic.
For these systems, anisotropy is defined by the Zener ratio, A:
C11  C12  / 2C44
or
2 S11  S12  / S44
A 

## Slide 61: FOR CUBIC SOLIDS
We can assume that most polycrystalline solids are isotropic but not all.
44
C C
C
 C11
0 
 

 

0 
0 
 

 
C12 C12 0 0 0 
11 12 0 0
 C11 0 0
   C 0 
     C44 0 
   

44 
44
S S
S
 S11
0 
 
0 
 

 
S12 S12 0 0 0 
 11 12 0 0 
   S11 0 0 0 
   S 0 
     S44 0 
   

44 
44
2
 C11  C22
C

44
11
22
S  2S  S

## Slide 62
Many parameters are used to describe the elastic properties of materials
See Ch. 8 in Nye, Ch. 13 in Newnham, or Ch. 10 in Gersten for a more thorough explanation.
Wikipedia also provides a nice discussion.
S11
E  1
S44
G  1  1
2 S11  S12 
S11
   S12
E
2 1 
G 
These expressions are for isotropic solids. They are interrelated

## Slide 63: Elastic Moduli in Cubic Materials
Where α, β, and γ are the direction cosines between the [hkl] crystal direction and the [100], [010], and [001] directions (i.e., the x,y,z axes).
α = cos([hkl][100]) ; β = cos([hkl][010]) ; γ = cos([hkl][010])
We can use the different relations among elastic constants to ascertain elastic moduli in any crystallographic orientation

2 2
    2 2   2 2 
11
11
12
1  S
2
hkl
E

 2  S  S  1 S

44 



## Slide 64
R.W. Hertzberg, Deformation & Fracture Mechanics of Engineering Materials, 4th ed., (John Wiley & Sons, New York, 1996) p. 14.

## Slide 65: Elastic properties of polycrystals
In single crystals elastic constants are determined by bonding between atoms. As such, most single crystals are mechanically anisotropic.
In polycrystals, the anisotropic behavior of each grain “averages out” because: (a) grain orientations tend to be random; and (b) the deformation of one grain is dependent on the deformation of its neighbor.
Exceptions occur when the material is textured (i.e., the grains exhibit a preferred orientation).
Page 34 in Hosford lists some possibilities.

## Slide 66
Elastic Waves in Cubic Crystals
Equation of Motion in X direction
Equations of Motion

## Slide 67
Waves in the [100] Direction
One solution is given by a longitudinal wave
the velocity /K of a longitudinal wave in the [100] direction is
Elastic Waves in Cubic Crystals

## Slide 68: Temperature dependence of elastic moduli
Young’s modulus does vary with temperature.
For metals and ceramics there are some general rules of thumb for temperatures lower than half of the melting temperature.
Different rules apply for polymers.

## Slide 69: Origin of T dependence
Repulsion
Attraction
ro
r
 |  | Ut
U
o
T = 0 K
T1 > 0 K
1
rT

## Slide 70
0
100
200
300
400
0
500 1000 1500 2000 2500 3000 3500
Re
W
Mo
Be
Fe
Mn Ni Cu
Al
Ag Au
Pb Mg
Zn
Sn Na
Ti
Cr
Zr
Nb
Ta
Ru
Ir
E (GPa)
500
Tmp (K)
Young’s modulus also tends to scale with Tmp for similar reasons.

## Slide 71: Influence of alloying
Alloying generally has little influence on the stiffness of materials. This is because the solubility of alloying elements is generally very small (<10%).
As noted by Roesler et al., the elastic modulus for Al alloys varies by roughly 10% while their strengths can be significantly altered by alloying.
The Cu-Ni system is an exception to the rule. Ni is 100% soluble in Ni.
121
207
[Roesler, p. 41]

## Slide 72
材料的弹性性质模拟

## Slide 73
Strain tensor
Stress tensor
Elastic constant
Stress-Strain relation

## Slide 74
Deformed
Unstrained
define the deformation; they are dimensionless and have values << 1 if the strain is small

## Slide 75
01
  确定平衡结构
0 K Lattice Relaxation
Finite Temperature NPT MD
03
计算Stress Tensor
基于经验势计算
05
构建 Strain Stress relation
02
通常是3个tensile、
3个 Shear
微扰晶胞
04
确定Strain tensor
注意Strain tensor 三个Shear 分量
重复02-05
求解弹性常数
最少需要六次
06
模拟流程

## Slide 76
1. 获取平衡结构
0 K - 晶胞优化
有限温度- NPT 分子动力学
1. 确定平衡结构

## Slide 77
2. 微扰晶胞
定义一个 deformation gradient 矩阵,
将与原始晶胞相乘得到deform以后的新晶胞，
以fcc为例，
注意： 微扰完晶胞需要对原子位置进行优化
0K 结构优化
有限温度 NVT 分子动力学
2. 微扰晶胞

## Slide 78
3. 计算 Stress Tensor
Numerical : Finite difference
Analytical : Depends on the energy functional
对晶格施加微小应变，计算应变后的总能量
计算 Stress Tensor：
在有限温度下，材料的能量对体积和晶格变形参数的导数可以得到应力张量的表达式。考虑到体积变形和剪切变形，应力张量的表达为：
其中， 是应变张量的分量
计算量较大，因为需要对系统进行多次微小扰动，每次扰动都需要重新计 算能量或力，因此计算速度较慢，且数值精度受限于微小扰动的大小。

## Slide 79
4. 确定 Strain Tensor
只关注形变影响，通过Green-Lagrange strain tensor的推导，我们可以得到，
放到小应变假设下，就可以省去二阶以上的高阶项，就有
小应变理论中的应变定义在连续介质力学中可以用变形梯度张量表示：
从而可以得到Strain Tensor的各个分量，继而得到Stress Tensor

## Slide 80
5. Stress - Strain relation
Stiffness张量通过弹性常数​将Stress分量与Strain分量关联起来
Strain分量 "ε" 和Stress分量 "σ" 由上述表达式通过一组方程联系起来,这些方程中的未知数是弹性常数。在下一步中,我们将收集更多这样的方程,直到我们拥有足够多的方程组来找到所有的。

## Slide 81
6. 求解弹性常数
使用彼此独立的deformation，直到完成6种deformation。任何6种deformation的组合都是可以的，只要它们是独立的
- 代表 tensile deformations， - 代表 shear deformation.

## Slide 82
为这6种deformation各自写出Stress-Strain relation，并将它们以矩阵形式表示。
在这个方程中要特别注意指标。在stress tensor 和 strain tensor 或中，这里ij作为index的含义，与我们至之前使用的ij含义不同。列指标 j 指的是Deformation的编号（第一次Deformation，第二次Deformation,...），而行指标 i 指的是在 Voigt表示法中的位置，如​是第四次变形的分量。
6. 求解弹性常数

## Slide 83
如果使用之前推荐的Deformation模式.则我们得到上式右边的矩阵,
这时我们只需要求解矩阵的逆。在上式左右两边同时乘以，我们就可以得到Stiffness tensor:
6. 求解弹性常数